## Slide 1: TRACKING THE DYNAMICS OF SYSTEMS EVOLVING THROUGH INFREQUENT TRANSITIONS IN A NETWORK OF DISCRETE STATES
Doros N. Theodorou
School of Chemical Engineering, Department of Materials Science and Engineering, National Technical University of Athens, Zografou Campus, 157 80 Athens, GREECE
doros@central.ntua.gr

## Slide 2: MOTIVATION
Atomistic molecular dynamics simulation: μs time scales. [see, however, ms-long simulations of K.Lindorff-Larsen, S. Piana, R.O. Dror, D.E. Shaw, Science 334, 517-520 (2011)].
Dynamics of most physical, chemical, materials, biological systems: s to years.
In many cases, dynamics is slow because the system spends most of its time trapped within relatively narrow regions of configuration space and only infrequently jumps from region to region.

## Slide 3: RUGGED ENERGY LANDSCAPES
x2
x1
Potential energy V (x), or
potential of mean force U(x)
Minima: “inherent structures” F. H. Stillinger, Science 267, 1935 (1995).
(Collections of) basins of attraction around minima: “states”.
The entire x-space can be tessellated into states.
atomic coordinate or collective variable (“order parameter”)

## Slide 4: EXAMPLES OF PHENOMENA INVOLVING EVOLUTION ON RUGGED ENERGY LANDSCAPES
Diffusion of defects and impurities in metals and semiconductors
Permeation of gas molecules through amorphous polymers
Diffusion of bulky hydrocarbons in zeolites
Structural relaxation and plastic deformation of glassy materials
Protein folding
Phase transitions in molecular and atomic clusters
Kinetics of networks of chemical reactions

## Slide 5: OUTLINE
Infrequent events, calculation of transition rate constants
Kinetic Monte Carlo simulation
The energy landscape picture for glasses
Low-temperature diffusion of Xe in Silicalite-1: Comparative application of various methods
A method for tracking structural relaxation in glasses: Application to atactic polystyrene
Master Equation: its analytical solution and calculation of time correlation functions
The lumping problem

## Slide 6: TRANSITION RATE CONSTANT
Time scale separation: Mean waiting time for transition out of a state is long in comparison with the time required for system to establish a restricted equilibrium among configurations in the state.
tcor << trxn
By the time it exits a state, the system has lost all memory of how it entered there (Markovian character of a sequence of infrequent events).
Rate constant kij: Probability per unit time that a transition to state j will occur, provided the system is in state i.

## Slide 7: COMPUTATION OF RATE CONSTANTS
Input: Energy hypersurface and masses associated with degrees of freedom.
Molecular dynamics (MD), reduction to an inherent structure trajectory and hazard plot analysis [E. Helfand, J. Chem. Phys. 69, 1010 (1978)]
Temperature-accelerated dynamics [M. R. Sørensen, A.F. Voter, J. Chem. Phys. 112, 9599 (2000)]
Transition-State Theory estimate from free energy difference between the system confined to the boundary hypersurface of state i and the system allowed to sample the entire state i. Calculation of dynamical correction factor through short MD trajectories initiated on the boundary hypersurface [C.H. Bennett, 1975; D. Chandler, J. Chem. Phys. 68, 2959 (1978), A.F. Voter and J.D. Doll, J. Chem. Phys. 82, 80 (1985)].

## Slide 8: COMPUTATION OF RATE CONSTANTS
Determination of reaction path (e.g., by Fukui’s intrinsic reaction coordinate approach) and computation of free energy profile along the path by umbrella sampling or “blue moon ensemble” simulations [T.R. Forester, W. Smith J. Chem. Soc. Faraday Trans. 93, 3249 (1997)]
Flux-tempered metadynamics [S. Singh, C.C. Chiu, J. de Pablo J. Stat. Phys. 144, 1 (2011); A. Laio, M. Parrinello, Proc. Natl. Acad. USA 99, 12562 (2002)]
Transition path sampling [P.G. Bolhuis, D. Chandler, C. Dellago, P.L. Geissler Annu. Rev. Phys. Chem. 53, 291 (2002); C. Dellago, P.G. Bolhuis, P. Geissler Adv. Chem. Phys. 123, 1 (2002)]

## Slide 9: CALCULATING RATE CONSTANTS FOR TRANSITIONS BETWEEN BASINS
Definitions:
Hazard rate h(t): Conditional probability that a system, which has survived a time t since its last transition, will undergo a transition between t and t+dt is h(t) dt.
Cumulative hazard H(t):
Probability that a transition occurs in time less than t since the last transition:
Poisson process: h(t) = λ, a constant. H(t)= λt, P(t)=1exp( λt)
Notes: P(t) = cumulative probability density function for residence times.
One has: 1-P(t+Δt) = [1-P(t)] [1-h(t)Δt]

## Slide 10: CALCULATING RATE CONSTANTS FOR TRANSITIONS BETWEEN BASINS
Hazard Plot Analysis Helfand, E. J. Chem. Phys. 69, 1010 (1978)
In the course of MD simulation, for any visited basin, β, record residence times between entry to and exit from the basin. Also record the basins γ to which exits from β occur.
Order residence times in β:
Estimate cumulative hazard corresponding to residence time tk:
Linear plot going through the origin indicates a Poisson process.
Slope of plot, λβ = total rate constant for exiting basin β.
Rate constant
Residence time tk (ps)
Notes: By definition, H(t) = -ln[1-P(t)]
with P(t) = probability for a transition out of the state to have occurred in time less than t.
Estimate of P(t) based on recorded transitions: P(t) = k/n
The sum on the right hand side of H^hat(t_k) can be viewed as an approximation of integral, from 0 to k/n , of 1/(1-x) dx.= -ln(1-k/n)

## Slide 11: SEQUENCE OF INFREQUENT EVENTS IS A HOMOGENEOUS POISSON PROCESS
Numbers of occurrences counted in disjoint time intervals are independent of each other.
Probability distribution of occurrences counted within any time interval only depends on the length of the interval.
No counted occurrences are simultaneous.
Waiting time until the next occurrence follows an exponential distribution:
Number of observed occurrences within a given time interval follows a Poisson distribution:
Several Poisson processes i occurring in parallel constitute a Poisson process with rate constant .

## Slide 12: KINETIC MONTE CARLO (KMC) SIMULATION
Generation of stochastic trajectories as sequences of transitions between states in a network of n states
Deploy N >> n independent walkers among the states according to a prescribed initial probability distribution: Ni (t) ≈ N Pi(0), i=1, 2, …, n
For each state i that is occupied at time t, calculate expected fluxes Ri→j(t) = Ni (t) ki→j , overall flux R(t) = ΣiΣjRi→j(t) and conditional probabilities qi→j(t) = Ri→j(t)/ R(t).
(ii) Pick time until next transition Δt=−ln(1ξ)/R(t), where ξ [0,1) is a uniformly distributed pseudorandom number. Pick type ij of next transition according to qi→j(t).
(iii) Of the Ni (t) walkers present in state i pick one with probability 1/ Ni (t) and move it to state j.
(iv) Advance simulation time by Δt. Update array keeping track of current positions of all walkers. Set Ni (t+ Δt) = Ni (t) − 1, Nj (t+ Δt) = Nj (t) + 1.
(v) Return to step (i).

## Slide 13: MASTER EQUATION
Pi(t): Probability of being in state i at time t.
j
ki→j
kj→i
i
or
Need to solve the master equation starting from an initial probability distribution among states P(0).
vector of state probabilities
Transition rate constant matrix
t→∞ : dP/dt=0, ki→j Pi(∞)= kj→i Pj(∞)
equilibrium state probabilities
(microscopic reversibility)

## Slide 14: MASTER EQUATION: ANALYTICAL SOLUTION
P(0) given
J. Wei, C.D. Prater, Advan. Catal. 13, 204 (1962).
N. V. Buchete, G. Hummer, J. Phys. Chem. B 112, 6057 (2008).
G. Boulougouris, DNT, J. Chem. Phys. 130, 044905 (2009).
K.E. Shuler, Phys. Fluids 2, 442 (1959).
Define reduced state probabilities:
given
Matrix is symmetric (microscopic reversibility)
Matrix is negative semidefinite
Real eigenvalues λ0=0 ≥ λ1 ≥ λ2 ≥ … ≥ λn-1
Eigenvector corresponding to λ0=0 is

## Slide 15: MASTER EQUATION: ANALYTICAL SOLUTION
J. Wei, C.D. Prater, Advan. Catal. 13, 204 (1962).
N. V. Buchete, G. Hummer, J. Phys. Chem. B 112, 6057 (2008).
G. Boulougouris, DNT, J. Chem. Phys. 130, 044905 (2009).
K.E. Shuler, Phys. Fluids 2, 442 (1959).
Diagonalization of permits writing down an analytical solution to the master equation.
Eigenvalues λ0=0 ≥ λ1 ≥ λ2 ≥ … ≥ λn-1
Eigenvectors
Orthonormality:
,
Solution of the master equation:

## Slide 16: EROPHILE: Eigenvalue Representation of Observables and Probabilities in a HIgh-dimensionaL Euclidean space
For any observable A, which has well-defined values Ai within each state i, nonequilibrium ensemble average value at time t is:
G. Boulougouris and DNT, J. Chem. Phys. 130, 044905 (2009)
∞: equilibrium among the n explored states.
Time autocorrelation function is:
where
Eigenvalues and eigenvectors of symmetrized n×n rate constant matrix describing transitions among n explored states (relaxation modes)

## Slide 17: EXAMPLE APPLICATION: LOW TEMPERATURE, LOW OCCUPANCY DIFFUSION OF XENON IN SILICALITE-1
Silicalite-1 (MFI)
Si96O192
Pnma
a = 20.07 Å
b = 19.91 Å
c = 13.42 Å
(3  3  3
unit cells shown)
y
x
z
Made up of SiO4 tetrahedra sharing vertices.
Straight and sinusoidal (zigzag) channels of diameter ≈ 5.5 Å

## Slide 18: Xe/SILICALITE-1, 300 Κ
MD simulation
E. Pantatosaki and G.K. Papadopoulos
Notes: 8 unit cells shown. Concentration 4 molecules per unit cell. 300Κ.

## Slide 19: TRANSITION STATE THEORY ANALYSIS OF Xe/Silicalite-1, 150 K
R.L June, A.T. Bell, and DNT J. Phys. Chem. 95, 8866 (1991)
S
Z
I
x
y
-a/4, b/2
-a/4, 0
a/4, 0
a/4, b/2
1
2
3
4
5
3
1
2
6
x
y
z
Notes: 8 unit cells shown. Concentration 4 molecules per unit cell. 300Κ.

## Slide 20
PI(∞) | 0.014
PS(∞) | 0.412
PZ(∞) | 0.574

## Slide 21: KINETIC MONTE CARLO

## Slide 22: KINETIC MONTE CARLO
Einstein, 1905

## Slide 23: SOLUTION OF THE MASTER EQUATION
Ld
. . . . . .
Cell 1
Cell 2
Cell 2ν -1
Cell 2ν
Cell 2ν-1 +1
Cell 2ν-1
2Lp
2ν unit cells n states/unit cell PBCs at the ends n=12, ν=7
• Direct diagonalization of 2νn 2νn matrix .
Approaches:
• Recursive reduction of dimensionality (MESoRReD), ultimately expressing the eigenvalues and eigenvectors of in terms of those of 2ν matrices of dimension nn, pertaining to the unit cell.
Panagiotis D. Kolokathis
• Numerical solution of the Master Equation by Euler method.
Initially only two central cells 2ν-1 and 2ν-1+1 filled, all others empty

## Slide 24: SOLUTION OF THE MASTER EQUATION
Ld
. . . . . .
Cell 1
Cell 2
Cell 2ν-1
Cell 2ν
Cell 2ν-1+1
Cell 2ν-1
2Lp
2ν unit cells n states/unit cell PBCs at the ends n=12, ν=7
P.D. Kolokathis
♦ 110-8 s
* 210-8 s
• 410-8 s
Points: MESoRReD
Line fits: continuum diffusion problem
Histograms: Euler method 110-8 s

## Slide 25
Dαα obtainable from nonzero eigenvalue of symmetrized rate constant matrix with smallest absolute magnitude.
Solution to Master Equation:
−λm (s−1)
Solution to Continuum Diffusion Equation:
Dxx ( fπ/Lp)2 (s−1)
Notes: Found a way to calculate lim_{L_p \rightarrow \infty} (- \lambda_1) by diagonalization of a matrix pertaining to a single unit cell. The matrix is an explicit function of \nu.

## Slide 26: Xe/Silicalite-1 at 150 K TST DIFFUSIVITIES FROM VARIOUS METHODS
Method | Dxx (10-10 m2 s-1) | Dyy (10-10 m2 s-1) | Dzz (10-10 m2 s-1) | D (10-10 m2 s-1)
KMC-TST1,2 | 9.67±0.14 | 11.62±0.25 | 1.71±0.05 | 7.66±0.14
Direct Diagonali-zation-TST, fit continuum soln.1 | 9.7088±0.0029 | 11.676±0.002 | 1.7627±0.0093 | 7.7157±0.0044
MESoRReD1-TST fit continuum soln. | 9.7088±0.0029 | 11.676±0.002 | 1.7627±0.0093 | 7.7157±0.0044
MESoRReD1-TST from λ1 | 9.7132 | 11.684 | 1.7531 | 7.7171
Euler Method1-TST | 9.70 | 12.5 | 1.83 | 8.01
KMC-DC TST2 | 5.1 | 7.3 | 0.83 | 4.41
MD2 | 4.3 | 10.0 | 0.99 | 5.1
PFG NMR3 | − | − | − | 1.6
2R.L. June, A.T. Bell, DNT J. Phys. Chem. 95, 8866 (1991)
3J Kärger, H. Pfeifer, F. Stallmach, N.N. Feoktistova, S.P. Zhdanov Zeolites 13, 50 (1993).
1P.D. Kolokathis and DNT, J. Chem. Phys. 137, 034112 (2012).

## Slide 27: Xe/Silicalite-1 at 150 K COMPUTATIONAL REQUIREMENTS
Method | CPU time (s) | Memory (MB)
KMC-TST1,2 | 6183.46 | 6
Direct Diagonalization-TST, fit continuum soln.1 | 37.81 | 38
MESoRReD1-TST, fit continuum soln. | 2.83 | 44
MESoRReD1-TST from λ1 | 0.0059 | 2
Euler Method1-TST | 23760 | 401
MD2 | 309173 | 
2R.L. June, A.T. Bell, DNT J. Phys. Chem. 95, 8866 (1991), normalized
1P.D. Kolokathis and DNT, J. Chem. Phys. 137, 034112 (2012).

## Slide 28: Xe/Silicalite-1 at 150 K COMPUTATIONAL REQUIREMENTS
Method | CPU time (s) | Memory (MB)
KMC-TST1,2 | 6183.46 | 6
Direct Diagonalization-TST, fit continuum soln.1 | 37.81 | 38
MESoRReD1-TST, fit continuum soln. | 2.83 | 44
MESoRReD1-TST from λ1 | 0.0059 | 2
Euler Method1-TST | 23760 | 401
MD2 | 309173 | 
2R.L. June, A.T. Bell, DNT J. Phys. Chem. 95, 8866 (1991), normalized
1P.D. Kolokathis and DNT, J. Chem. Phys. 137, 034112 (2012).

## Slide 29: Xe/Silicalite-1 at 150 K COMPUTATIONAL REQUIREMENTS
Method | CPU time (s) | Memory (MB)
KMC-TST1,2 | 6183.46 | 6
Direct Diagonalization-TST, fit continuum soln.1 | 37.81 | 38
MESoRReD1-TST, fit continuum soln. | 2.83 | 44
MESoRReD1-TST from λ1 | 0.0059 | 2
Euler Method1-TST | 23760 | 401
MD2 | 309173 | 
2R.L. June, A.T. Bell, DNT J. Phys. Chem. 95, 8866 (1991), normalized
1P.D. Kolokathis and DNT, J. Chem. Phys. 137, 034112 (2012).

## Slide 30: GLASSES ARE NON-EQUILIBRIUM MATERIALS
J. Hadač, P. Slobodian, P. Říha, P. Sáha, R.W. Rychwalski, I. Emri, J. Kubát, J. Non-Cryst. Solids, 353, 2681-2691 (2007)
atactic Polystyrene (aPS)
Mw=145 kg/mol
Mw/Mn=1.03
LIQUID
GLASS
Glass structure and properties depend on the rate of cooling from the melt.

## Slide 31: GLASSES ARE NON-EQUILIBRIUM MATERIALS
J. Hadač, P. Slobodian, P. Říha, P. Sáha, R.W. Rychwalski, I. Emri, J. Kubát, J. Non-Cryst. Solids, 353, 2681-2691 (2007)
aPS, Mw=145 kg/mol, Mw/Mw=1.03, Tg(1oC/min)=97.8±0.2oC
Glass properties change with time (physical ageing)

## Slide 32: GLASSES ARE NON-EQUILIBRIUM MATERIALS WITH COMPLEX MECHANICAL BEHAVIOUR
PC in compression: Effect of ageing
H. Van Melick, Ph.D. Thesis, Technical University of Eindhoven, 2002

## Slide 33: ENERGY LANDSCAPE-BASED MODELING OF GLASSY ATACTIC POLYSTYRENE
Starting point: Well-equilibrated melt configurations
T. Spyriouni, C. Tzoumanekas, DNT, G. Milano, F. Müller-Plathe, Macromolecules, 40, 3876-3885 (2007).

## Slide 34: Segmental Dynamics and Glass Transition: atactic Polystyrene
Fit to empirical Williams–Landel–Ferry relation [1]:
Ferry, J. D. “Viscoelastic Properties of Polymers”, 3rd ed. Wiley, New York, 1980.
Hintermeyer, J. et al. Macromolecules 2008, 41, 9335.
Experimental Tg [2] : 373 K
Vogiatzis G.G.; DNT Macromolecules 2014, 47, 387.
Atomistic Molecular Dynamics

## Slide 35: Energy Landscape Picture of a Glass
Configuration fluctuating in the neighborhood of local energy minima: “Inherent structures” : Stillinger, F.H. Science 1995, 267, 1935. See also work by P.G. Debenedetti, D.J. Lacks, A. Heuer, G. Parisi, F. Sciortino, D. Wales, T. Keyes, T.M. Truskett, DNT and U.W. Suter.
Transitions between minima inhibited by high energy barriers.
Glass properties: arithmetic averages of properties of individual “basins of attraction”. Restricted equilibrium established within each basin.
Glassy computer specimens generated by rapid cooling of the melt.
V
Metabasin
Inherent structure
x
Basin
(C. Dellago)
Notes: Quasi-harmonic approximation within basins

## Slide 36: In-basin motion: Quasi-Harmonic Approximation (QHA)
V (x0) =Vinh and i are functions of the spatial extent of the system.
Eigenvalue problem
Second derivatives of the potential energy
Mass-weighted coordinates
Normal mode angular frequencies
Helmholtz energy

## Slide 37: GIBBS ENERGY MINIMIZATION OF A BASIN UNDER GIVEN STRESS STATE
Quench from melt by classical MD
Vk= Vo,…,Vf
Gk(T, P, Vk)
Vibrational free energy
Inherent structure
Atactic polystyrene modified A.Lyulin et al. (2003) model isotropic dilation/contraction
N.P. Kopsias and DNT, J. Chem. Phys. 109, 8573 (1998). D. Tsalikis, G.C. Boulougouris, DNT.

## Slide 38: Volumetric Behavior: QHA vs. MD
Atactic polystyrene, modified A.Lyulin* model
Pressure 1 bar
MD cooling rate 0.5 K/ns
641 united atoms
Averages over 5 basins
Exp: Zoller, P.; Walsh, D.J. Standard Pressure-Volume-Temperature Data for Polymers. Technomic: Lancaster, 1995.
*Lyulin, A.V.; DeGroot, J.; Michels, M. Macromol. Symp. 2003, 191, 167.
Lempesis, N.; Vogiatzis, G.G.; Boulougouris, G.C.; van Breemen, L.C.A.; Hütter, M.; DNT, Mol. Phys. 2013, 111, 3430.
Notes: Debye temperature around 100 K

## Slide 39: Elasticity of Polymer Glasses: Quasi-harmonic approximation
Glassy atactic polystyrene (PS) | Computation | Experiment
Young’s modulus E (GPa), 300 K | 3.55 | 3.2-3.7
dE/dT (MPa/K) | -6.0 | -4.48
Poisson ratio ν | 0.35 | 0.33
dν/dT (K-1) | 0.00022 | 0.00015
200 computational “specimens”, p=1 bar
Lempesis, N; Vogiatzis, G.G.; Boulougouris, G.C.; van Breemen, L.C.A.; Hütter, M.; DNT, Mol. Phys. 2013, 111, 3430.

## Slide 40: Relaxation in glasses: Energy landscape picture
A
network topology
energy landscape
B
B
C
C
D
D
Determine saddle points out of initial basin A.
Discover new minima
Through each saddle point, determine reaction path
Calculate transition rates
A
‡

## Slide 41: ELEMENTARY TRANSITIONS BETWEEN BASINS
First step on either side in the direction of the eigenvector correspon- ding to the negative eigenvalue of the Hessian:
Subsequent steps in steepest descent direction:
Through each saddle point, determine reaction path “Intrinsic Reaction Coordinate”, K. Fukui Acc.Chem.Res. 14, 363 (1981).
Determine saddle points (1, 2, 3, 4, …) out of current basin A. “Dimer method”, G. Henkelmann and H. Jónsson, J. Chem. Phys. 111, 7010 (1999).
Estimate transition rate constants via Transition State Theory
Quasi-harmonic approximation
‡
‡

## Slide 43
Chart: Euclidean norm (position vector)
Energy profile along an elementary transition
a-PS, T=250 K ,P = 1 bar, β=1/(kBT)
, Å
V

## Slide 44
Explored
Boundary
“Dynamical Integration of a Markovian Web” (DIMW): G. Boulougouris and DNT, J. Chem. Phys. 127, 084903 (2007)
TRACKING THE EVOLUTION OF THE PROBABILITY DISTRIBUTION
AMONG STATES BASED ON A FIRST PASSAGE SAMPLING SCHEME
Distinguish between “explored” states (paths leading out of them determined), and “boundary” states (connected to explored states but not yet explored themselves).
Set of explored states augmented by appending a boundary state at an appropriately chosen time based on first passage time analysis.
Set of boundary states updated by including neighbours of newly added state.
Analytical solution of master equation, with atomistically calculated rate constants, in a network of states that is progressively augmented “on the fly”
Time-dependent probability of occupancy of each explored state determined by analytical solution of master equation:

## Slide 45: Creating a network of states
Graph representation: Vogiatzis, G.G.; van Breemen L.C.A.; Hütter, M. Macromol. Theor. Simul. 2019, 190036.