## Slide 1: KINETIC MONTE CARLO

## Slide 2: KINETIC MONTE CARLO
Einstein, 1905

## Slide 3: SOLUTION OF THE MASTER EQUATION
Ld
. . . . . .
Cell 1
Cell 2
Cell 2ν -1
Cell 2ν
Cell 2ν-1 +1
Cell 2ν-1
2Lp
2ν unit cells n states/unit cell PBCs at the ends n=12, ν=7
• Direct diagonalization of 2νn 2νn matrix .
Approaches:
• Recursive reduction of dimensionality (MESoRReD), ultimately expressing the eigenvalues and eigenvectors of in terms of those of 2ν matrices of dimension nn, pertaining to the unit cell.
Panagiotis D. Kolokathis
• Numerical solution of the Master Equation by Euler method.
Initially only two central cells 2ν-1 and 2ν-1+1 filled, all others empty

## Slide 4: SOLUTION OF THE MASTER EQUATION
Ld
. . . . . .
Cell 1
Cell 2
Cell 2ν-1
Cell 2ν
Cell 2ν-1+1
Cell 2ν-1
2Lp
2ν unit cells n states/unit cell PBCs at the ends n=12, ν=7
P.D. Kolokathis
♦ 110-8 s
* 210-8 s
• 410-8 s
Points: MESoRReD
Line fits: continuum diffusion problem
Histograms: Euler method 110-8 s

## Slide 5
Dαα obtainable from nonzero eigenvalue of symmetrized rate constant matrix with smallest absolute magnitude.
Solution to Master Equation:
−λm (s−1)
Solution to Continuum Diffusion Equation:
Dxx ( fπ/Lp)2 (s−1)
Notes: Found a way to calculate lim_{L_p \rightarrow \infty} (- \lambda_1) by diagonalization of a matrix pertaining to a single unit cell. The matrix is an explicit function of \nu.

## Slide 6: Xe/Silicalite-1 at 150 K TST DIFFUSIVITIES FROM VARIOUS METHODS
Method | Dxx (10-10 m2 s-1) | Dyy (10-10 m2 s-1) | Dzz (10-10 m2 s-1) | D (10-10 m2 s-1)
KMC-TST1,2 | 9.67±0.14 | 11.62±0.25 | 1.71±0.05 | 7.66±0.14
Direct Diagonali-zation-TST, fit continuum soln.1 | 9.7088±0.0029 | 11.676±0.002 | 1.7627±0.0093 | 7.7157±0.0044
MESoRReD1-TST fit continuum soln. | 9.7088±0.0029 | 11.676±0.002 | 1.7627±0.0093 | 7.7157±0.0044
MESoRReD1-TST from λ1 | 9.7132 | 11.684 | 1.7531 | 7.7171
Euler Method1-TST | 9.70 | 12.5 | 1.83 | 8.01
KMC-DC TST2 | 5.1 | 7.3 | 0.83 | 4.41
MD2 | 4.3 | 10.0 | 0.99 | 5.1
PFG NMR3 | − | − | − | 1.6
2R.L. June, A.T. Bell, DNT J. Phys. Chem. 95, 8866 (1991)
3J Kärger, H. Pfeifer, F. Stallmach, N.N. Feoktistova, S.P. Zhdanov Zeolites 13, 50 (1993).
1P.D. Kolokathis and DNT, J. Chem. Phys. 137, 034112 (2012).

## Slide 7: Xe/Silicalite-1 at 150 K COMPUTATIONAL REQUIREMENTS
Method | CPU time (s) | Memory (MB)
KMC-TST1,2 | 6183.46 | 6
Direct Diagonalization-TST, fit continuum soln.1 | 37.81 | 38
MESoRReD1-TST, fit continuum soln. | 2.83 | 44
MESoRReD1-TST from λ1 | 0.0059 | 2
Euler Method1-TST | 23760 | 401
MD2 | 309173 | 
2R.L. June, A.T. Bell, DNT J. Phys. Chem. 95, 8866 (1991), normalized
1P.D. Kolokathis and DNT, J. Chem. Phys. 137, 034112 (2012).

## Slide 8: Xe/Silicalite-1 at 150 K COMPUTATIONAL REQUIREMENTS
Method | CPU time (s) | Memory (MB)
KMC-TST1,2 | 6183.46 | 6
Direct Diagonalization-TST, fit continuum soln.1 | 37.81 | 38
MESoRReD1-TST, fit continuum soln. | 2.83 | 44
MESoRReD1-TST from λ1 | 0.0059 | 2
Euler Method1-TST | 23760 | 401
MD2 | 309173 | 
2R.L. June, A.T. Bell, DNT J. Phys. Chem. 95, 8866 (1991), normalized
1P.D. Kolokathis and DNT, J. Chem. Phys. 137, 034112 (2012).

## Slide 9: Xe/Silicalite-1 at 150 K COMPUTATIONAL REQUIREMENTS
Method | CPU time (s) | Memory (MB)
KMC-TST1,2 | 6183.46 | 6
Direct Diagonalization-TST, fit continuum soln.1 | 37.81 | 38
MESoRReD1-TST, fit continuum soln. | 2.83 | 44
MESoRReD1-TST from λ1 | 0.0059 | 2
Euler Method1-TST | 23760 | 401
MD2 | 309173 | 
2R.L. June, A.T. Bell, DNT J. Phys. Chem. 95, 8866 (1991), normalized
1P.D. Kolokathis and DNT, J. Chem. Phys. 137, 034112 (2012).

## Slide 10: GLASSES ARE NON-EQUILIBRIUM MATERIALS
J. Hadač, P. Slobodian, P. Říha, P. Sáha, R.W. Rychwalski, I. Emri, J. Kubát, J. Non-Cryst. Solids, 353, 2681-2691 (2007)
atactic Polystyrene (aPS)
Mw=145 kg/mol
Mw/Mn=1.03
LIQUID
GLASS
Glass structure and properties depend on the rate of cooling from the melt.

## Slide 11: GLASSES ARE NON-EQUILIBRIUM MATERIALS
J. Hadač, P. Slobodian, P. Říha, P. Sáha, R.W. Rychwalski, I. Emri, J. Kubát, J. Non-Cryst. Solids, 353, 2681-2691 (2007)
aPS, Mw=145 kg/mol, Mw/Mw=1.03, Tg(1oC/min)=97.8±0.2oC
Glass properties change with time (physical ageing)

## Slide 12: GLASSES ARE NON-EQUILIBRIUM MATERIALS WITH COMPLEX MECHANICAL BEHAVIOUR
PC in compression: Effect of ageing
H. Van Melick, Ph.D. Thesis, Technical University of Eindhoven, 2002

## Slide 13: ENERGY LANDSCAPE-BASED MODELING OF GLASSY ATACTIC POLYSTYRENE
Starting point: Well-equilibrated melt configurations
T. Spyriouni, C. Tzoumanekas, DNT, G. Milano, F. Müller-Plathe, Macromolecules, 40, 3876-3885 (2007).

## Slide 14: Segmental Dynamics and Glass Transition: atactic Polystyrene
Fit to empirical Williams–Landel–Ferry relation [1]:
Ferry, J. D. “Viscoelastic Properties of Polymers”, 3rd ed. Wiley, New York, 1980.
Hintermeyer, J. et al. Macromolecules 2008, 41, 9335.
Experimental Tg [2] : 373 K
Vogiatzis G.G.; DNT Macromolecules 2014, 47, 387.
Atomistic Molecular Dynamics

## Slide 15: Energy Landscape Picture of a Glass
Configuration fluctuating in the neighborhood of local energy minima: “Inherent structures” : Stillinger, F.H. Science 1995, 267, 1935. See also work by P.G. Debenedetti, D.J. Lacks, A. Heuer, G. Parisi, F. Sciortino, D. Wales, T. Keyes, T.M. Truskett, DNT and U.W. Suter.
Transitions between minima inhibited by high energy barriers.
Glass properties: arithmetic averages of properties of individual “basins of attraction”. Restricted equilibrium established within each basin.
Glassy computer specimens generated by rapid cooling of the melt.
V
Metabasin
Inherent structure
x
Basin
(C. Dellago)
Notes: Quasi-harmonic approximation within basins

## Slide 16: In-basin motion: Quasi-Harmonic Approximation (QHA)
V (x0) =Vinh and i are functions of the spatial extent of the system.
Eigenvalue problem
Second derivatives of the potential energy
Mass-weighted coordinates
Normal mode angular frequencies
Helmholtz energy

## Slide 17: GIBBS ENERGY MINIMIZATION OF A BASIN UNDER GIVEN STRESS STATE
Quench from melt by classical MD
Vk= Vo,…,Vf
Gk(T, P, Vk)
Vibrational free energy
Inherent structure
Atactic polystyrene modified A.Lyulin et al. (2003) model isotropic dilation/contraction
N.P. Kopsias and DNT, J. Chem. Phys. 109, 8573 (1998). D. Tsalikis, G.C. Boulougouris, DNT.

## Slide 18: Volumetric Behavior: QHA vs. MD
Atactic polystyrene, modified A.Lyulin* model
Pressure 1 bar
MD cooling rate 0.5 K/ns
641 united atoms
Averages over 5 basins
Exp: Zoller, P.; Walsh, D.J. Standard Pressure-Volume-Temperature Data for Polymers. Technomic: Lancaster, 1995.
*Lyulin, A.V.; DeGroot, J.; Michels, M. Macromol. Symp. 2003, 191, 167.
Lempesis, N.; Vogiatzis, G.G.; Boulougouris, G.C.; van Breemen, L.C.A.; Hütter, M.; DNT, Mol. Phys. 2013, 111, 3430.
Notes: Debye temperature around 100 K

## Slide 19: Elasticity of Polymer Glasses: Quasi-harmonic approximation
Glassy atactic polystyrene (PS) | Computation | Experiment
Young’s modulus E (GPa), 300 K | 3.55 | 3.2-3.7
dE/dT (MPa/K) | -6.0 | -4.48
Poisson ratio ν | 0.35 | 0.33
dν/dT (K-1) | 0.00022 | 0.00015
200 computational “specimens”, p=1 bar
Lempesis, N; Vogiatzis, G.G.; Boulougouris, G.C.; van Breemen, L.C.A.; Hütter, M.; DNT, Mol. Phys. 2013, 111, 3430.

## Slide 20: Relaxation in glasses: Energy landscape picture
A
network topology
energy landscape
B
B
C
C
D
D
Determine saddle points out of initial basin A.
Discover new minima
Through each saddle point, determine reaction path
Calculate transition rates
A
‡

## Slide 21: ELEMENTARY TRANSITIONS BETWEEN BASINS
First step on either side in the direction of the eigenvector correspon- ding to the negative eigenvalue of the Hessian:
Subsequent steps in steepest descent direction:
Through each saddle point, determine reaction path “Intrinsic Reaction Coordinate”, K. Fukui Acc.Chem.Res. 14, 363 (1981).
Determine saddle points (1, 2, 3, 4, …) out of current basin A. “Dimer method”, G. Henkelmann and H. Jónsson, J. Chem. Phys. 111, 7010 (1999).
Estimate transition rate constants via Transition State Theory
Quasi-harmonic approximation
‡
‡

## Slide 23
Chart: Euclidean norm (position vector)
Energy profile along an elementary transition
a-PS, T=250 K ,P = 1 bar, β=1/(kBT)
, Å
V

## Slide 24
Explored
Boundary
“Dynamical Integration of a Markovian Web” (DIMW): G. Boulougouris and DNT, J. Chem. Phys. 127, 084903 (2007)
TRACKING THE EVOLUTION OF THE PROBABILITY DISTRIBUTION
AMONG STATES BASED ON A FIRST PASSAGE SAMPLING SCHEME
Distinguish between “explored” states (paths leading out of them determined), and “boundary” states (connected to explored states but not yet explored themselves).
Set of explored states augmented by appending a boundary state at an appropriately chosen time based on first passage time analysis.
Set of boundary states updated by including neighbours of newly added state.
Analytical solution of master equation, with atomistically calculated rate constants, in a network of states that is progressively augmented “on the fly”
Time-dependent probability of occupancy of each explored state determined by analytical solution of master equation: